## Slide 1: Castrol Tribol GR SW 460-1
Component failure from axial loading and contact fatigue are serious problems for wind turbine bearings. Main bearing failure alone accounts for $180,000 in repair costs, 80 man hours, and potentially weeks of lost production for each occurrence. In addition, long re-lubrication intervals make it hard to resist false brinelling and fretting corrosion. Production from a wind turbine also requires operation in difficult ambient conditions: from blistering heat to frigid cold.
DESIGNED to meet THE
MANY challenges faced
by wind turbines
CHALLENGES FACED BY WIND TURBINES
Difficult environmental conditions
Slow speeds and shock loading from erratic wind patterns
Extremely long re-lubrication intervals
Failures caused by sliding and axial loading in addition to false brinelling and fretting corrosion
An ideal solution would be a lubricant that’s not only longer lasting, but that can also provide protection under these challenging conditions*.
And if that lubricant could meet multiple specifications for use across a range of applications, that’s means there’s even less to worry about.
That lubricant exists – meet Castrol Tribol GR SW 460-1.
*Based on various lab tests, versus the leading competitors. For more details refer to the relevant sales presenter.

## Slide 2: INTRODUCING CASTROL TRIBOL GR SW 460-1
CUSTOM-DESIGNED FOR WIND TURBINES
Tribol GR SW 460-1 with MFT-PD technology*
Withstands high/shock loads
Resists shearing and wear (fretting, rolling, sliding)
Resists water ingress and corrosion
Good mobility at low temperatures for easy start up
Low friction – improves energy efficiency and prolongs component life
Controlled bleed rate and oil separation
One grease to meet the multiple challenges faced by wind turbines
Difficult environmental conditions
Extremely long re-lubrication intervals
Failure caused by sliding, axial loading, vibration, fretting corrosion and false brinelling
Multiple test protocols and specifications

## Slide 3: Active mft-pd protection
Castrol tribol gr sw 460-1
Conventional lubricants use sacrificial additives that get used up and need to be replenished. So even though they protect equipment, there’s still wear – and breakdowns still happen.
Castrol’s new wind turbine grease, Tribol GR SW 460-1 takes a completely different approach using Microflux Trans plastic deformation technology – or MFT-PD. It actively smoothens the surface, without depositing or removing material.
That means less pressure, less friction and less wear. Since MFT-PD is non-sacrificial and needs replacing less frequently, re-lubrication intervals can be longer. So, the result is not only increased protection and lower maintenance, but lower energy and lubricant costs, too.
PROTECTIVE LAYER FORMS IMMEDIATELY
PROTECTIVE LAYER COMPRESSED, REDUCING FRICTION
PROTECTION
COMPRESSION
MICROSMOOTHING
ADDITIVES MIGRATE INTO METAL SURFACE
STAGE
1
STAGE
2
STAGE
3
MAKING MAIN BEARINGS LAST LONGER
Mechanically stable, Castrol Tribol GR SW 460-1 protects bearings against corrosion, withstands high loads and shock loads, and resists shearing, wear and water ingress. That means contact areas in critical components are significantly smoother, wear from false brinelling is drastically reduced and run in time is shorter.

## Slide 4: DESIGNED SPECIFICALLY FOR WIND TURBINE USE:
CASTROL TRIBOL GR SW 460-1 TOP IN LAB TESTS
PROPERTY | TEST DESCRIPTION | METHOD | PARAMETER | TRIBOL GR SW 460-1 | GOOD | MEDIUM | POOR
MECHANICAL STABILITY | Roll Stability Test (50 h, 80 °C) | ASTM D1831 mod | PW 60 unit change | < 10 % | < 15 % | 15 - 20 % | > 20 %
CORROSION RESISTANCE | Emcor Test 1 % NaCl | DIN 51802 |  | ≤ 0 / 1 | ≤ 0 / 1 | 1 / 1 – 1 / 2 | > 1 / 2
LOW TEMPERATURE | Flow Pressure at -40 °C | DIN 51805 |  | 525 hPa | ≤ 800 hPa | 825 - 1400 hPa | > 1400 hPa
 | Low Temp Torque at -40 °C | ASTM D1478 | Start Torque (ST) / Running Torque (RT) | 0.3 Nm / 0.07 Nm | < 0.5 Nm / < 0.1 Nm | 0.5-1.0 Nm / 0.1-0.5 Nm | > 1.0 Nm / > 0.5 Nm
FE8 – WEAR | FE8 C/75/50 | DIN 51819-2 | Wear MW50 | 1.5 mg | < 10 mg | 10 - 50 mg | > 50 mg
FE8 – TEMP/TORQUE | FE8 C/75/50 | DIN 51819-2 | Temperature max ST / RT | < 50 °C 12 Nm / 5.5 Nm | < 60 °C <15 Nm / <8 Nm | 60 - 90 °C 15 -30 Nm / 8 - 15 Nm | > 90 °C > 30 Nm / > 15 Nm
FAFNIR – ASTM D4170 |  | ASTM D4170 | Wear loss | < 10 mg | < 10 mg | 10– 20 mg | > 20 mg
SRV – ASTM D7594 |  | ASTM D7594 | COF Friction curve | Low, stable Smooth, no fretting | Low, stable Smooth, no fretting | Medium, stable Smooth, no fretting | High, unstable Rocky, fretting
SRV – ASTM D7594 at 0 °C |  | ASTM D7594 | COF Friction curve | Stable, no fretting | Stable, no fretting | N/A | Rocky, fretting

## Slide 5: DESIGNED SPECIFICALLY FOR WIND TURBINE USE:
PROPERTY | TRIBOL GR SW 460-1 | COMPETITOR A | COMPETITOR B | COMPETITOR C | COMPETITOR D | COMPETITOR E
MECHANICAL STABILITY |  |  |  |  |  | 
CORROSION RESISTENCE |  |  |  |  |  | 
LOW TEMPERATURE |  |  |  |  |  | 
FE8 – WEAR |  |  |  |  |  | 
FE8 – TEMP/TORQUE |  |  |  |  |  | 
FAFNIR – ASTM D4170 |  |  |  |  |  | 
SRV – ASTM D7594 |  |  |  |  |  | 
SRV – ASTM D7594 at 0 °C |  |  |  |  |  | 
CASTROL TRIBOL GR SW 460-1 TOP IN LAB TESTS
RELATIVE PERFORMANCE RATING |  | 
GOOD | MEDIUM | POOR