## Slide 1
CASTROL HYSOL SL 30 XBB
Semi-synthetic metalworking fluid provides improved machining performance for ferrous alloys
TM

## Slide 2
CONTENTS
WHO WE ARE – CASTROL & BP
1
  Castrol and BP
  Our heritage
METALWORKING FLUIDS
2
  Current market trends
  What do you expect from your coolants?
  Requirements from customers and distributors
CASTROL’S SOLUTION
3
  Castrol Hysol SL 30 XBB
  Application guidance and technical data
CASE STUDIES
4
  Proven in field (Case Studies)
LAB TEST RESULTS
5
Overview
Alkalinity
Microbiology challenge test
Foaming properties – CNOMO
Hard-water stability
Foaming properties – SITA
Recirculation test
Residue test
Corrosion protection
Tapping
BUS-MODEL: Skin Compatibility

## Slide 3
SECTION 1
WHO WE ARE

## Slide 4
WHO WE ARE – CASTROL & BP
CASTROL
Castrol (BP Lubricants) was founded in 1899 by Charles Cheers Wakefield
We operate directly in over 46 countries
We market our products to over half a million customers in 120 countries
We employ 7,500 people worldwide
BP
BP is one of the world’s leading international oil and gas companies
We employ over 74,500 people
We have operations on six continents and in over 80 countries

## Slide 5: CASTROL: A SPECIALIST LUBRICANTS BUSINESS AND PART OF BP
WHO WE ARE – CASTROL & BP
BP delivers energy products and services to people around the world.
FINDING
OIL AND GAS
DEVELOPING
AND EXTRACTING
OIL AND GAS
TRANSPORTING
AND TRADING
OIL AND GAS
MANUFACTURING
FUELS AND PRODUCTS
MARKETING
FUELS AND
PRODUCTS
INTERNATIONAL OIL
AND GAS MARKETS
FUELS, LUBRICANTS AND PETROCHEMICALS
GENERATING RENEWABLE ENERGY
UPSTREAM
DOWNSTREAM

## Slide 6: OUR TECHNOLOGY AND MANUFACTURING CENTRES FOR INDUSTRIAL PRODUCTS
WHO WE ARE – CASTROL & BP
WARMINSTER, PENNSYLVANIA
NAPERVILLE, ILLINOIS
MUMBAI, INDIA
SHANGHAI, CHINA
MELBOURNE, AUSTRALIA
LANDAU, GERMANY
MÖNCHENGLADBACH, GERMANY
PÉRONNE, FRANCE
PANGBOURNE, UK
Production centre
Technology centre
TAICANG, CHINA
NAGOYA, JAPAN

## Slide 7
To remain competitive, manufacturers are increasingly focused on eliminating waste and inefficiencies
Stricter legislation can increase cutting fluid disposal costs, and can limit the use of chemicals once widely used in manufacturing
Choosing the optimum cutting fluid is key in helping to future-proof production
Manufacturing industries are constantly under pressure to improve their operational processes
Machining excellence cannot be compromised
Current Market Trends
What do you expect from your coolants?
Have a long life (e.g. it does not become contaminated rapidly)
Perform well and meet specifications
Provide product consistency – to specification, every time
Works well and prevents downtime across different metal types
Be eco-friendly
Not require excessive usage of biocides to keep it fresh
Does not cause problems with machines or with personnel (e.g. skin irritation)

## Slide 8
Requirements from customers and distributors
Improved anti-corrosion performance and pH stability
Low foam in soft and hard water conditions
Meet current and future regulatory requirements for health, safety and waste treatment
Suitable across ferrous alloys (like cast iron) machining

## Slide 9
HYSOL SL 30 XBB
Semi-Synthetic Metalworking Fluid
Overcome the severe requirements of foam, long emulsion stability and anti-corrosion performance
Formulated without boron, DCHA, formaldehyde releasing agent, and monoethanolamine.

## Slide 10
Application Guidance and Technical Data of Hysol SL 30 XBB
 | Cast Iron | Low alloyed steel | High alloyed stainless steel | Aluminum Alloys | Yellow Metals
Grinding | • • | • • | • • |  | 
Milling, turning (general machining) | • • | • • | • |  | 
Drilling | • • | • • |  |  | 
Reaming, tapping | • • | • |  |  | 
Broaching | • • | • |  |  | 
• Possible application, please consult Castrol representative prior to use • • Suggested core application |  |  |  |  | 
Concentrate | 
Mineral oil [%] | 30
EP/AW-Additive | Yes (P)
Boron/Formaldehyde | Free
Emulsion | 
Appearance | Translucent to Milky
pH-value (4 %) | 9,7
Grinding 4-6%
General Machining 5-10%
Water range 200-800 ppm CaCO3

## Slide 11
Hysol SL 30 XBB vs. Standard Cast Iron Coolant
Hysol SL 30 XBB
3% = 0/1
4% = 0/0
Standard Cast Iron Coolant
3% = 1/1
4% = 0/0
Chip Corrosion Test – DIN 51360/2 20°dH (CIP 507-02)

## Slide 12
Hysol SL 30 XBB vs. Standard Cast Iron Coolant
Conclusion After 7 Days on 3 samples
Standard Cast Iron Coolant: Significant corrosion at all concentrations
Hysol SL 30 XBB: No corrosion at all concentrations (partly slightly corrosion on 1 of 3 panels per concentration)
The Q-Panels were cleaned with benzine.
One side was polished with Aluminium oxide cloth 240 grid.
The panels were submerged in emulsion for one minute and dried at room temperature for 20-60 minutes.
The panels were placed in a Weiss WK 111 humidity chamber at 48°C and 90% relative humidity for 7 days
Humidity Chamber Testing, 5% in VE
Slightly Corrosion Visible
Hysol SL 30 XBB
Standard Cast Iron Coolant
No Corrosion Visible
No Corrosion Visible
Corrosion Visible

## Slide 13
Aluminium and Yellow Metal Compatibilty
Test Conditions:
6% Emulsion of Hysol SL 30 XBB
in 100 ppm CaCO3, room temperature
Test duration of 48 hours
Brass
ADC12
6063
Cu
Hysol SL 30 XBB
7075
Brass
ADC12
6063
Cu
Standard Cast Iron Coolant
7075

## Slide 14
Alkalinity 4% in 20 °dH
Chart: ml HCL 0.1
Hysol SL 30 XBB
Standard Cast Iron Coolant
Product | Start pH-value | pH 7 - ml HCl (0.1M) | pH 8 - ml HCl (0.1M)
Standard Cast Iron Coolant | 9.7 | 61 | 45
Hysol SL 30 XBB | 9.6 | 60 | 44

## Slide 15
Microbiology Testing
 | Days |  |  |  |  |  |  |  |  | 
Product | 3 | 7 | 10 | 14 | 17 | 21 | 24 | 28 | PID 1 | PID3
Hysol SL 30 XBB | 0,00E+00 | 0,00E+00 | 0,00E+00 | 1,00E+03 | 0,00E+00 | 1,00E+03 | 0,00E+00 | 2,00E+04 | 1,00E+03 | 0,00E+00
Standard Cast Iron Coolant | 1,00E+02 | 0,00E+00 | 0,00E+00 | 0,00E+00 | 0,00E+00 | na | 0,00E+00 | 0,00E+00 | 0,00E+00 | 0,00E+00
 | Days |  |  |  |  |  |  |  |  | 
Product | 3 | 7 | 10 | 14 | 17 | 21 | 24 | 28 | PID1 | PID3
Hysol SL 30 XBB | 0,00E+00 | 0,00E+00 | 0,00E+00 | 0,00E+00 | 0,00E+00 | 0,00E+00 | 0,00E+00 | 0,00E+00 | 0,00E+00 | 0,00E+00
Standard Cast Iron Coolant | 0,00E+00 | 0,00E+00 | 0,00E+00 | 0,00E+00 | 0,00E+00 | na | 0,00E+00 | 1,00E+01 | 0,00E+00 | 0,00E+00
Bacteria
Fungi
Internal microbiology challenge test over a 4-week period (5%, 200 ppm)
Product | Start | 1st Week | 2nd Week | 3rd Week | End | (Start-End)
Hysol SL 30 XBB | 9,50 | 9,24 | 9,30 | 9,17 | 9,18 | -0,32
Standard Cast Iron Coolant | 9,51 | 9,36 | 9,49 | 9,37 | 9,38 | -0,13
pH-Value

## Slide 16
SITA foam test – 6% 100ppm, CIP 514-06
After 24h emulsions were filtered (8µM) and again a SITA foam test was performed.
Chart: Measuring cycle - run 3
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20
Hysol SL 35 XBB | 6 | 241 | 268 | 295 | 296 | 288 | 298 | 302 | 298 | 298 | 307 | 304 | 306 | 301 | 302 | 308 | 309 | 308 | 310 | 303 | 314
LD 0147 SC | 4 | 332 | 367 | 383 | 396 | 400 | 398 | 407 | 409 | 412 | 411 | 410 | 411 | 411 | 415 | 413 | 412 | 415 | 416 | 415 | 414
Hysol SL 35 XBB filtered | 59 | 333 | 349 | 367 | 376 | 388 | 394 | 405 | 401 | 409 | 415 | 415 | 427 | 422 | 429 | 431 | 431 | 435 | 435 | 436 | 436
LD 0147 SC filtered | 1 | 341 | 399 | 415 | 431 | 448 | 452 | 450 | 457 | 458 | 458 | 462 | 460 | 464 | 464 | 463 | 464 | 462 | 461 | 464 | 463
Chart: time (s)
| 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 110 | 120 | 130 | 140 | 150 | 160 | 170 | 180 | 190 | 200 | 210 | 220 | 230 | 240 | 250 | 260 | 270 | 280 | 290 | 300
Hysol SL 35 XBB | 314 | 234 | 214 | 200 | 178 | 166 | 147 | 134 | 122 | 108 | 97 | 89 | 82 | 76 | 68 | 64 | 57 | 51 | 44 | 39 | 34 | 30 | 27 | 24 | 22 | 20 | 18 | 17 | 15 | 14 | 13
LD 0147 SC | 414 | 397 | 384 | 356 | 321 | 283 | 245 | 210 | 176 | 142 | 109 | 79 | 55 | 37 | 24 | 16 | 12 | 10 | 8 | 7 | 6 | 6 | 6 | 6 | 5 | 5 | 5 | 5 | 4 | 4 | 4
Hysol SL 35 XBB filtered | 436 | 428 | 421 | 416 | 411 | 406 | 398 | 392 | 386 | 381 | 375 | 369 | 361 | 353 | 347 | 337 | 333 | 325 | 315 | 307 | 299 | 290 | 281 | 270 | 262 | 254 | 244 | 238 | 228 | 219 | 212
LD 0147 SC filtered | 463 | 448 | 441 | 430 | 397 | 364 | 333 | 303 | 275 | 245 | 215 | 183 | 154 | 126 | 98 | 72 | 50 | 30 | 17 | 11 | 7 | 5 | 5 | 4 | 3 | 3 | 2 | 2 | 1 | 1 | 1
Standard Cast Iron Coolant
Hysol SL 30 XBB
Standard Cast Iron Coolant filtered
Hysol SL 30 XBB filtered
Hysol SL 30 XBB filtered
Standard Cast Iron Coolant
Hysol SL 30 XBB
Standard Cast Iron Coolant filtered

## Slide 17
CNOMO Foam Test
6% Emulsion, 100ppm (CIP1004), Emulsion tested without defoamer in the concentrate
Chart: time in min
| 0.5 | 1 | 2 | 4 | 22 | 28
Hysol SL 35 XBB - Day 1 | 140 | 160 | 140 | 180 | 800 | 1000
Hysol SL 35 XBB - Day 2 | 140 | 180 | 180 | 220 | 220 | 240 | 380 | 730 | 860 | 1000
LD 0147 SC - Day 1 | 320 | 420 | 520 | 600 | 700 | 750 | 820 | 770 | 770 | 710 | 680 | 690 | 670 | 670 | 670
LD 0147 SC - Day 2 | 180 | 180 | 180 | 180 | 180 | 560 | 700 | 710 | 700 | 700 | 700
Chart: time in min
| 0 | 0.5 | 1 | 2 | 3 | 4 | 5 | 12
Hysol SL 35 XBB - Day 1 | 1000 | 940 | 780 | 380 | 200 | 140 | 100 | 0
Hysol SL 35 XBB - Day 2 | 1000 | 920 | 760 | 480 | 300 | 180 | 140 | 80 | 0
LD 0147 SC - Day 1 | 670 | 630 | 500 | 160 | 70 | 20 | 5 | 0
LD 0147 SC - Day 2 | 700 | 700 | 650 | 320 | 120 | 40 | 20 | 5 | 0
Standard Cast Iron Coolant Day 1
Standard Cast Iron Coolant Day 2
Hysol SL 30 XBB Day 1
Hysol SL 30 XBB Day 2

## Slide 18
Recirculation Test (in house Renault)
 | Day 1 | Day 2 | Day 3 | Day 4 | Day 5 | Day 8
Water hardness / Nozzle | Tap water (12°dH) No nozzle | Tap water (12°dH) Nozzle 1 | Tap water (12°dH) Nozzle 0.5 | 35°dH Nozzle 0.5 | 50°dH Nozzle 0.5 | 50°dH Nozzle 0.5
Emulsion Appearance | good; nearly no foam, less soaps on surface 1 g soaps | good; big foam bubbles, fast decay 1.4 g soaps | good; less foam than day 2, fast decay 0.3 g soaps | good; nearly no foam, fast decay 0.3 g soaps | good, nearly no foam, fast decay 2 g soaps | Good, no oil, no creme, low foam, small layer of soaps 22 g soaps
Day 1
Day 5
Day 2
Day 3
Day 4 (before run)
Day 8
Bath: 5% 25l
No oil/no split
Hysol SL 30 XBB

## Slide 19
Recirculation Test (in house Renault)
Hysol SL 30 XBB
Day 1
Day 5
Day 2
Day 3
Day 4 (before run)
Day 8
Product passes test, when these criteria are met:
- no overflow
- no emulsion split
- total soap amount below 80 g (here: 27g)

## Slide 20
Emulsion Appearance (4%) after foam shaking test,
CIP 514-01
No significant differences in foam height and foam decay between both products
Standard Cast Iron Coolant (directly)
Hysol SL 30 XBB (directly)
5°dH 20°dH 40°dH 60°dH
5°dH 20°dH 40°dH 60°dH
5°dH 20°dH 40°dH 60°dH
5°dH 20°dH 40°dH 60°dH
Standard Cast Iron Coolant (48h)
Hysol SL 30 XBB (48h)

## Slide 21
Emulsion compatibility
With Standard Cast Iron Coolant
Emulsions: 20°dH 4%
directly: picture was taken after foam shaking test
after 24h: foam shaking test was repeated, afterwards picture was taken
directly
after 24h
1 2 3 4 5
 | Standard Cast Iron Coolant | Hysol SL 30 XBB
1 | 100% | 0%
2 | 75% | 25%
3 | 50% | 50%
4 | 25% | 75%
5 | 0% | 100%

## Slide 22
Results Reichert- wear test
CIP 525
wear: 1,5kg
10% emulsion
DI water
Product | Wear surface [mm2] | Noise meter [m]
Hysol SL 30 XBB | 26 | >100
Standard Cast Iron Coolant | 29 | >100

## Slide 23
Skin Compatibility
The BUS* skin model
Conclusion: Based on the score evaluation after an open topical application (exposure period: 0.5hrs, 1.0hr, 5.0hrs, 1x appl.; unstripped skin) it can be concluded that the product Hysol SL 30 XBB (fresh; 20%) is non-irritant to the skin, even after repeated skin contact.
* Bovine Udder Skin (isolated perfused udder skin)
(Kietsmann et al. 1993)
INVESTIGATION METHODS
Analytical Method
Skin biopsy, Histoshaver (skin sections), Horny layer strippings, Dermatome cuts,
Perfusion liquid
Biochemical Method
Cytotoxicity: e.g. MTT, Inflammatory mediators: e.g. PGE2, enzymes:
e.g. LDH, SDH (V-max)
Morphological Method
Histology, scanning electron microscopy, V-max method
APPLICATION
Epidermis
Dermis
Cutis
TEST MATERIAL
Pharma, cosmetics, household/industry chemicals, working materials, medical devices
Open/occlusive
2 x 600–800cm2
PENETRATION, PERMEATION, ABSORPTION
Dr. Wolfgang F. Pittermann, Certified Veterinary Pathologist
Lab Test Results

## Slide 24
PLEASE CONTACT:
TM